MET 443 COMPOSITE MATERIALS

CATALOG DATA:

MET 443 COMPOSITE MATERIALS (3-0) 3 credits. Prerequisites: ME 316 or concurrent enrollment in MET 440. The course will cover heterogeneous material systems; basic design concepts and preparation; types of composite materials; advances in filaments, fibers and matrices; physical and mechanical properties; failure modes; thermal and dynamic effects; and applications to construction, transportation and communication. This course is cross-listed with ME 443.

TEXTBOOK:

Engineering Mechanics of Composite Materials, 2nd Edition, Daniel and Ishai, Oxford 2006

INSTRUCTORS:

Dr. Jon J. Kellar, Office Hours: 2-3 pm M, Tu, W, Th

Dr. Lidvin Kjerengtroen, Office Hours, 2-3 pm M, Tu, W, Th

REQUIRED/ELECTIVE:

MET 443 is a Directed Technical Elective for B.S. Metallurgical Engineering students.

COURSE OBJECTIVE:

Students will be able to determine the effects of mechanics and materials chemistry on composite performance.

COURSE OUTCOMES:

- Given a particular matrix/reinforcement combination students will be able to identify a manufacturing process to produce a desired composite part.

- Given one of the major fibrous reinforcements the students will be able to describe the design, manufacturing and properties of advanced fibers.

- For a given matrix/reinforcement systems students will be able to determine the role of interfaces and interface phases and their properties in the design, manufacture and properties of PMCs, MMCs and CMCs.

- For a given matrix/reinforcement system student will be able to predict the microstructural properties (stiffness, strength, fracture toughness and fatigue).

- For a given composite system the student will be able to describe the fundamental properties/parameters such as anisotropic, orthotropic, and non-homogenous material behavior.

- For a given composite system the student will be able to carry out two dimensional transformations of stress, strain, and directional elastic parameters.

- For a given set of constituent properties the student will be able to estimate laminate material properties including laminate properties and strength estimates using common failure criteria.

- Given a laminate system the student will have basic understanding of the assumptions of laminate behavior and the significance of laminate stacking order.

TOPICS COVERED:

- Fibers

- Fibers and Whiskers and Nanocomposites

- Reinforcement/Matrix Interface

- Interfaces-Wettability

- Interfaces-Bonding

- The Interphase Methods for Measuring Bond Strength

- Polymer Matrices

- Polymer Matrix Composite Processing

- Polymer Matrix Composite Interfaces/Interphases

- Structure, Properties and Applications of PMCs

- Elastic behavior of composite lamina-Micromechanics

  - Basic concepts including RVE

  - Stiffness

  - Thermal and moisture expansion

  - Lamina Strength

- Ply Mechanics

  - Coordinate systems

  - Stress, strain, and constitutive relationships

  - Off-axis Stiffness and properties

- Macro Mechanics

  - Basic assumptions of laminates

  - Computation of stress

  - Common laminate types: symmetric, balanced, and quasi-isotropic, and specially orthotropic

  - Carpet plots

- Failure and Strength

  - Tsai-Hill

  - Tsai-Wu

  - Maximum Strain Criterion

CLASS SCHEDULE:

Lecture: 3 hours per week, 1:00-1:50 am, MWF

RELATIONSHIP OF COURSE TO PROGRAM OUTCOMES: (a), (c)

LABORATORY:

There is no associated laboratory with this course.

CONTRIBUTION OF COURSE TO MEETING THE PROFESSIONAL COMPONENT:

This course prepares students in the basics of materials selection and design.

Ethical practice is a frequent discussion item in MET 443, specifically, the role engineer’s play in selection of materials for critical applications such as defense, crash protection and aerospace.

One major design report is a required part of this course.

PERSON WHO PREPARED THIS DESCRIPTION AND DATE OF PREPARATION:

Jon Kellar and Lidvin Kjerengtroen, May 6, 2010